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BONDING SYSTEM


One‑Component, Thermal Cure

Epoxy MF7

One-Part Epoxy Adhesive

Description:
Epoxy MF7 is an epoxy‑based heat activated adhesive. This product have been designed to be used for those applications that require the convenience of a one-part system as well as the speed of cure more typically found in two part chemistries. Epoxy system MF7  bonds well to most metals and engineered plastics and it provides excellent resistance to moisture and conventional cleaning solvents. 

The Epoxy MF7 adhesive system exhibits more flexibility and a higher impact strength than the Epoxy MF5.  

Uncured Properties:

Composition:
Epoxy

Viscosity @ 25C                                75,000 cps

Color:
Black

Flash Point:
> 200°F

Toxicity:
Low

Specific Gravity:
1.20

Cured Properties:

Hardness, Shore D:
52

Elongation, % :
22

Moisture Resistance:
Excellent

Operating Temperature Range, °C:
‑50 to 140

Cure Overview:

This product can be cured at any one of the following schedules:

60 minutes at 100C   or

30 minutes at 120C   or

5 minutes at 150C     or

2 minutes at  180C

Shelf-Life & Storage:

Epoxy MF7 will provide a greater than 30 day stability at room temperature. When product is not in use it can be stored for up to 6 months at temperatures below 5C.

Ellsworth Adhesive Systems makes no express or implied warranties or merchantability, fitness or otherwise with respect to this product. In addition, while the information contained herein is believed to be reliable, no warranty is expresses or implied regarding the accuracy of the results to be obtained from the use thereof. The properties given are typical values and are not intended for use in preparing specifications. User should make their own test to determine the suitability of this product for their own purposes.


